CONFIDENTIAL // FOR INTERNAL REFINERY RELIABILITY USE ONLY

EMERGENCY TECHNICAL APPROVAL NOTE - CDU TRANSFER LINE

| SUBJECT: | Sanction for Ultrasonic NDT Verification & Segment Replacement on Pipeline #PL-4820-A |
| --- | --- |
| DATE & TIME: | 2026-09-27 06:04 UTC |
| SECURITY CLASSIFICATION: | SOVEREIGN AIR-GAPPED ASSET INTEGRITY |
| APPROVAL ROUTE: | Chief General Manager (Inspection & Reliability) / Asset Integrity Lead |

1. BACKGROUND & INCIDENT CONTEXT

During scheduled turnaround inspection at CDU-101 Unit 04, ultrasonic wall thickness surveying identified localized thinning at elbow junction EB-04B.

2. STATUTORY REFERENCES & APPLICABLE SOPS

[SOP-INS-2025, Page 18, Section 4.2]

[IR-2026-8924 Dated 24-Sep-2026]

API-570 Piping Inspection Code

3. DETAILED INSPECTION FINDINGS & NDT MEASUREMENTS

Ultrasonic wall thickness measured at 3.42 mm (Nominal: 9.52 mm).

Statutory MAWT is 4.50 mm. Calculated absolute deficit is 1.08 mm (24.0% below limit).

Severe localized pitting corrosion observed on outer bend radius due to naphthenic acid/H2S exposure.

4. TECHNICAL & STRUCTURAL ASSESSMENT

The component has exceeded statutory safe operating life. Continued pressurized operation at 28.5 Bar poses imminent risk of hydrocarbon containment loss.

5. ESTIMATED FINANCIAL IMPACT & WORK ORDER BUDGET

Estimated repair, fabrication, NDT, and emergency mechanical overhaul cost: $35,500.

6. RISK RATING & CONTAINMENT MATRIX

CRITICAL PRIORITY - Immediate bypass isolation and 48-hour mechanical replacement mandatory.

7. ENGINEERING RECOMMENDATIONS

Approve Emergency Work Order WO-REF-9021 for Schedule 80 ASTM A106-B elbow spool fabrication.

8. APPROVAL & SIGN-OFF DIRECTIVE

Recommended for immediate sanction: Chief General Manager (Inspection & Reliability) / Asset Integrity Lead

| Prepared By: Reliability AI | Verified By: Chief Inspector | Approved By: CGM (Operations) |
| --- | --- | --- |
| _______________________ Date: _______________ | _______________________ Date: _______________ | _______________________ Date: _______________ |